Synthesis of ZIF-8 (ACS-catalysis):

Equipment needed:
Glass beaker (250 ml)
Vials w/cap (20 ml) x 8
Oven

Chemicals:
1.	Zinc Nitrate hexahydrate (Zn(NO2)3 6 H2O)
2.	2-methylimidazole (H-MeIM)
3.	N,N'-dimethylformamide (DMF)
4.	Chloroform
5.	dichlormethane

Protocol:
Solid mixture of 1 (1.88g, 6.33 mmol) and 2 (0.43g, 5.82 mmol) dissolved in 130 ml of 3 and distributed in 20 ml vials. Vials are capped tightly before heating at 5C/min untill 140 C and held at this temp for 24 hours and then cooled at 0.4 C/min to room temperature. Remove mother liquid and add 4 (20 ml), collect crystals from upper layer. Wash crystals with 3 (3 x 15 ml) for 3 days, then with 5 (3 x 15 ml) for 3 days. Remove residual solvents by heating in vacuum to 200 C for 6 hours. Product should be white polyhedra.

Synthesis of ZIF-8 at room temp:

Equipment:

Synthesis of ZIF-4 (Cambridge)

Equipment needed:
Autoclave
Hirch-funnel